The design, construction, and maintenance of stormwater management facilities are governed by the specifications included in Section 9.4 of the Henrico County Environmental Compliance Manual.  The following checklist only identifies the information and details that must be included in the SWM plan.

VA DEQ DESIGN SPEC. NO. 4:  SOIL COMPOST AMENDMENTS

Used in conjunction with:

Rooftop Disconnection:	BMP  Identifier:_

Filter Strip:			BMP  Identifier:_

Grass Channel:		BMP  Identifier:_

MINIMUM DESIGN CRITERIA:

- Material specifications must be included on the construction plans.

The compost must be derived from plant material and provided by a member of the U.S. Composting Seal of Testing Assurance (STA).

The compost must be the result of biological degradation and transformation of plant-derived materials under conditions that promote anaerobic decomposition.

The compost must have a moisture content that has no visible free water or dust when handling the materials.

The compost must meet the following criteria, as reported by the U.S. Composting Seal of Testing Assurance (STA):

100% of the material passes through a ½ inch screen;

The pH is between 6 and 8;

Manufactured inert material is less than 1% by weight;

The organic matter content is between 35% and 65%;

Soluble salt content is less than 6 mmhos/cm;

Maturity is greater than 80%;

Stability is 7 or less;

The carbon/nitrogen ratio is less than 25:1;

The trace material test result is “pass”;

The dry bulk density is between 40 lbs./cu. ft. and 50 lbs./cu. ft.

ADDITIONAL COMMENTS:

PLAN REQUIREMENTS:

- Provide a site map identifying the following information:

The topographical information;

A soil map for the site and area of the facility;

Soil boring locations, if necessary;

Show the layout and dimensions of the soil amended area.

- The plans must clearly indicate that the SWM facility has been designed in accordance with Section 9.4.4 (Soil Amendments) of the Henrico County Environmental Compliance Manual.

ADDITIONAL COMMENTS:

CONSTRUCTION:

- The sequence of construction must address the SWM facility installation and appropriate inspections, including:  initial site preparation, excavation/grading, and installation of the embankment, principal outlet structure, and emergency spillway.  We recommend the County staff be involved in these inspections.

- The sequence of construction must address the following:

Specify two soil tests (pre-construction 1 ft. down and 1 week after amendments have been incorporated) be provided in the following manner:

Deep tilling to a depth of 12-18 inches is needed after the final building lots have been graded.

The appropriate compost mix will be incorporated into the soil using a rototiller or similar equipment at a volumetric rate of 1 part compost to 2 parts soil.

The soil amendment area must be identified and protected during construction.

- The sequence of construction must clearly state that a construction record drawing and certification that the stormwater management facility has been constructed in accordance with the approved plan must be submitted to the County and approved prior to Environmental Compliance Bond (ECB) release.

ADDITIONAL COMMENTS:

Reviewed by:

Date Reviewed:

Phone Number:

July 2014